| SAFETY ALERT |
| --- |
| SYSTEM/ EQUIPMENT | Freight wagon series Habis, Number 33 80 2753 843-2, VKM: TWA – TRANSWAGGON AB |
| SAFETY ISSUE DESCRIPTION | The railway undertaking SŽ – Tovorni promet informed Slovenian NSA about crack on the bogie frame of the unloaded freight wagon. The crack was detected during the train inspection (train number: 45084). |
| CIRCUMSTANSES (e.g. special weather conditions) | The safety issue was spotted at the railway station Sežana (Slovenia) on 29.7.2019. The freight wagon was unloaded during the inspection. It was removed from the traffic. |
| REASON FOR ISSUE | The cause cannot be determined precisely, it is suspected that the damage may have been due to a defect in the material or a structural defect or to the action of forces released during transport. Indicated cracks refer to the wagons type Habbis. It is recommended to conduct inspections of all vehicles from this type regarding possible cracks on bogie frames. Irregularities related to the technical condition of wagons should be immediately reported to the ECM and manufacturer. |
| LIST OF SUPPORTING DOCUMENTS (e.g. PHOTOS, LINKS) | Information about vehicle type, photographic documentation of the cracks, wagon damage report. |
| LINKED WITH OCCURRENCE NOTIFIED TO ERA DATABASE? | no | LINK TO ERA NOTIFICATION - |
|  | OCCURRENCE DATE - |  |

| ISSUER |
| --- |
| ORGANISATION | Public Agency of the Republic of Slovenia for Railway Transport – NSA in Slovenia |
| CONTACT DATA |  | +386 (0)2 234 14 27 |  | gp.azp@azp.si |
| ISSUE DATE | 07/08/2019 |